12/11/2021 12:52:01

20211112EDX

Click here to enter text.

Project Notes

Specimen 7


Click here to enter text.

Specimen Notes for 'Specimen 7'


Site 2

Click here to enter text.

Site Notes for 'Site 2'



|  |  |
| --- | --- |
| Label: | Electron Image 15 |
| Collected: | 12/11/2021 12:51:57 |
| Input Signal: | SE |
| Resolution (Width): | 1024 pixels |
| Resolution (Height): | 768 pixels |
| Pixel Size: | 0.05855 µm |
| Image Width: | 60μm |
| Image Height: | 45μm |
| Accelerating Voltage: | 2.00kV |
| Magnification: | 2000 x |
| Working Distance: | 7.0mm |
| Stage X: | 7.395mm |
| Stage Y: | -7.277mm |
| Stage Z: | 7.276mm |
| Stage Tilt Degrees: | 0.00° |
| Specimen Tilt Degrees: | 0.00° |
| Software Tilt Correction: | Not applied |
| Stage Rotate: | 0.0° |
| Number of Averaged Frames: | 1 |
| Dwell Time: | 1μs |



|  |  |
| --- | --- |
| Label: | Spectrum 16 |
| Source: | Acquired |
| Created: | 12/11/2021 12:52:01 |
| Livetime: | 99.9s |
| Process Time: | 6 |
| Accelerating Voltage: | 2.00kV |
| Magnification: | 2000 x |
| Working Distance: | 7.0mm |
| Stage X: | 7.395mm |
| Stage Y: | -7.3mm |
| Stage Z: | 7.3mm |
| Stage Tilt: | 0.00° |
| Specimen Tilt (degrees): | 0.00 |
| Stage Rotate: | 0.0° |
| Elevation (degrees): | 21.0 |
| Azimuth (degrees): | 0.0 |
| Number Of Channels: | 4096 |
| Energy Range (keV): | 10 keV |
| Energy per Channel (eV): | 2.5eV |
| Detector Type: | Ultim Extreme |
| Detector Type Id: | 64 |
| Window Type: | None |
| Pulse Pile Up Correction: | Succeeded |
| Primary Detector: | Extreme |
| Primary Detector Serial Number: | UVA9045 |

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| **Spectrum 16** |  |  |  |  |
| Element | Line Type | Wt% | Wt% Sigma | Atomic % |
| C | K series | 3.84 | 0.06 | 16.07 |
| O | K series | 17.78 | 0.20 | 55.84 |
| Ce | M series | 78.37 | 0.24 | 28.10 |
| Total: |  | 100.00 |  | 100.00 |