## Slide 1
strength
Buildability
Sports Sand
PFA
Building Sand
Plasticiser
Silica fume
Silica flour
Egg albumen
Foam
w/b ratio 0.36-0.50
w/b ratio <0.35
RMA:
hemc,
Xanthan
gum
CEM1
Chart: 
| Sand | CEM1 | PFA | Water | HEMC | Xan | Plast. | Foam
160518 (S/B 0.40, W/B 0.48) | 20.9565 | 34.0543 | 18.337 | 24.6239 | 0.28108 | 0.56976 | 0.52391 | 0.66851
Chart: 
| Sand | CEM1 | PFA | Water | HEMC | Xan | Plast. | Foam
060318 3 (W/B 0.47) | 0 | 43.8185 | 23.5946 | 31.01 | 0.29122 | 0.61885 | 0.67413 | 0
Workability
Buildability
a
b
c
d
Workability
G* (MPa)
Ffk (MPa)
δ (°)
Force/10 (N)
Force/10 (N)
Fck (MPa)
Ffk (MPa)
Ffk (MPa)
Fck (MPa)
Ffk (MPa)
Fck (MPa)
Fck (MPa)
δ (°)
δ (°)
δ (°)
G* (MPa)
G* (MPa)
G* (MPa)
Force/10 (N)
Force/10 (N)
0
10
20
30
40
50
(W/B 0.50, S/B 0.40)
(W/B 0.47)
(W/B 0.48)
(W/B 0.48, S/B 0.40)
100
102
104
106
108
Material viscosity η – while at rest
η - while in the vessel
η – while in the tube
10-4
102
10-2
100
Mix 1
Mix 2
Mix 3
Mix 4
Chart: 
| Sand | CEM1 | PFA | Water | HEMC | Xan | Plast. | Foam
290418 (W/B 0.48) | 0 | 43.1854 | 23.2537 | 31.2264 | 0.27627 | 0.53766 | 0.66439 | 0.8404
Chart: 
Force | 34.2299 | 47.8327 | 52.3468 | 56.1197
Fc | 26.9612 | 24.6413 | 19.35 | 22.785
Ff | 3.2818 | 6.93 | 3.7707 | 4.3429
G* | 4.6488 | 6.7416 | 4.6848 | 8.1335
ᵟ | 18.3924 | 3.6951 | 2.2751 | 1.6953
Chart: Shear Rate (1/s)
Syringe shear rate | 1 | 100000000
Tube shear rate | 1 | 100000000
at rest | 1 | 100000000
Chart: 
| Sand | CEM1 | PFA | Water | HEMC | Xan | Plast. | Foam
170418 (S/B 0.40, W/B 0.50) | 20.7391 | 33.7011 | 18.1467 | 25.4054 | 0.27977 | 0.51537 | 0.51848 | 0.67734