## Slide 1
Chart: Compressive Strength (MPa) Length (m)
| 060318 3 maze | 060318 3 wall | 060318 3 hybrid
Strength - 7 day compressive | 16.542 | 14.3684 | 25.7222
Length of 4 full circular layers | 11.7088 | 15.2161 | 13.5726
Strength per linear cm - 2 layers | 2.8256 | 1.8886 | 3.7903
e
b
d
25mm
Maze
Wall
Hybrid
Maze
Hybrid
Wall
c
Maze
Hybrid
Wall
a
80mm
25mm