| Label: | Electron Image 2 |
| --- | --- |
| Collected: | 19/11/2020 12:49:09 |
| Input Signal: | SE |
| Resolution (Width): | 2048 pixels |
| Resolution (Height): | 1536 pixels |
| Pixel Size: | 0.00586 µm |
| Image Width: | 12μm |
| Image Height: | 8.99μm |
| Accelerating Voltage: | 3.00kV |
| Magnification: | 10000 x |
| Working Distance: | 7.0mm |
| Stage X: | 5.809mm |
| Stage Y: | -3.835mm |
| Stage Z: | 8.072mm |
| Stage Tilt Degrees: | 0.00° |
| Specimen Tilt Degrees: | 0.00° |
| Software Tilt Correction: | Not applied |
| Stage Rotate: | 360.0° |
| Number of Averaged Frames: | 1 |
| Dwell Time: | 5μs |

| Label: | Map Sum Spectrum |
| --- | --- |
| Source: | Acquired |
| Created: | 19/11/2020 12:49:33 |
| Livetime: | 167.1s |
| Process Time: | 4 |
| Accelerating Voltage: | 3.00kV |
| Magnification: | 10000 x |
| Working Distance: | 7.0mm |
| Stage X: | 5.809mm |
| Stage Y: | -3.8mm |
| Stage Z: | 8.1mm |
| Stage Tilt: | 0.00° |
| Specimen Tilt (degrees): | 0.00 |
| Stage Rotate: | 360.0° |
| Elevation (degrees): | 21.0 |
| Azimuth (degrees): | 0.0 |
| Number Of Channels: | 1024 |
| Energy Range (keV): | 10 keV |
| Energy per Channel (eV): | 10.0eV |
| Detector Type: | Ultim Extreme |
| Detector Type Id: | 64 |
| Window Type: | None |
| Pulse Pile Up Correction: | Succeeded |
| Primary Detector: |  |
| Primary Detector Serial Number: | UVA9045 |

| Label: | EDS Layered Image 3 |
| --- | --- |
| Collected: | 19/11/2020 12:49:33 |
| Resolution (Width): | 2048 pixels |
| Resolution (Height): | 1536 pixels |
| Pixel Size: | 0.00586 µm |
| Image Width: | 12μm |
| Image Height: | 8.99μm |
| Accelerating Voltage: | 3.00kV |
| Magnification: | 10000 x |
| Working Distance: | 7.0mm |
| Stage X: | 5.809mm |
| Stage Y: | -3.835mm |
| Stage Z: | 8.072mm |
| Stage Tilt Degrees: | 0.00° |
| Specimen Tilt Degrees: | 0.00° |
| Software Tilt Correction: | Not applied |
| Stage Rotate: | 360.0° |
| Primary Detector: |  |
| Primary Detector Serial Number: | UVA9045 |

| Map Sum Spectrum |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Element | Line Type | Apparent Concentration | k Ratio | Wt% | Wt% Sigma | Standard Label | Factory Standard | Standard Calibration Date |
| C | K series | 36.52 | 0.36516 | 3.84 | 0.05 | C Vit | Yes |  |
| O | K series | 957.02 | 3.22046 | 25.40 | 0.08 | SiO2 | Yes |  |
| Si | K series | 8.28 | 0.06558 | 0.55 | 0.10 | SiO2 | Yes |  |
| Cu | L series | 636.00 | 6.36004 | 67.44 | 0.13 | Cu | Yes |  |
| Ge | L series | 21.66 | 0.21661 | 2.77 | 0.09 | Ge | Yes |  |
| Total: |  |  |  | 100.00 |  |  |  |  |